| - GENERAL |  |
| --- | --- |
| 1.1 SECTION INCLUDES | Materials and installation of polymeric geotextiles used in retaining wall structures, filtration, drainage structures, roadbeds and Yard areas purpose of which is to: Separate and prevent mixing of granular materials of different grading. Act as hydraulic filters permitting passage of water while retaining soil strength of granular structure. |
| 1.2 CITY SPECIFICATIONS AND RELATED SECTIONS | City of Winnipeg Standard Construction Specifications: CW 3170 – Earthwork and Grading CW 3130 – Supply and Installation of Geotextile Fabrics. .2 Related Sections Section 31 23 33.01 – Excavating, Trenching and Backfilling. Section 32 91 19.13 – Topsoil Placement and Grading Section 33 46 20 – Foundation and Under-slab Drainage Section G2020 – Yard and Parking Lot |
| 1.3 REFERENCES | .1 CW 3130 - Supply and Installation of Geotextile Fabrics .2 Canadian General Standards Board (CGSB) CAN/CGSB-4.2 No. 11.2-[M89(April 1997)], Textile Test Methods - Bursting Strength - Ball Burst Test (Extension of September 1989). CAN/CGSB-148.1, Methods of Testing Geotextiles and Complete Geomembranes. No.2-M85, Methods of Testing Geosynthetics - Mass per Unit Area. No.3-M85, Methods of Testing Geosynthetics - Thickness of Geotextiles. No.6.1-93, Methods of Testing Geotextiles and Geomembranes - Bursting Strength of Geotextiles Under No Compressive Load. |
| SUBMITTALS | .1 Submit samples in accordance with Section 01 33 00 - Submittal Procedures. |
| 1.5 DELIVERY, STORAGE AND HANDLING | During delivery and storage, protect geotextiles from direct sunlight, ultraviolet rays, excessive heat, mud, dirt, dust, debris and rodents. |
| - PRODUCTS |  |
| MATERIAL | Geotextile: non-woven synthetic fibre fabric, supplied in rolls, as per CW 3130. Securing pins and washers: to CAN/CSA-G40.21, Grade 300W, hot-dipped galvanized with minimum zinc coating of 600 g/m² to CAN/CSA G164. Factory seams: sewn in accordance with manufacturer's recommendations. Thread for sewn seams: equal or better resistance to chemical and biological degradation than geotextile. |
| - EXECUTION |  |
| INSTALLATION | As per CW 3130. Place and compact soil layers in accordance with Section 31 23 33.01 - Excavating Trenching and Backfilling, and 33 46 20 - Foundation and Under-slab Drainage. |
| CLEANING | Remove construction debris from project site and dispose of debris in an environmentally responsible and legal manner. |
| PROTECTION | Vehicular traffic not permitted directly on geotextile. |